## Slide 1: Sheet Metal Forming Processes

## Slide 2
The ease with which a sheet can be formed into a specific shape without fracture/excessive thinning.
Formability is controlled by the material properties: Strain hardening exponent (n), Anisotropy coefficient (R) and Strain rate sensitivity index (m)
Why Formability?
Personal communication with Prof. R. Dashwood, Univ. of Warwick and Prof. J.W. Yoon of Deakin Univ., and Banabic et. al., 2000, Formability of Metallic Materials
Localized necking
autobody
Aircraft structures
Home appliances
Splitting
2

## Slide 3: Common sheet metal operations
stretching
deep drawing
bending
blanking and piercing
coining
Ironing
A complex stamping is formed by combination of the above processes.

## Slide 4
A schematic showing common sheet metal forming operations

## Slide 5: Stretching
In-plane stretching
Out-of-plane stretching
Formability measure
Limiting dome height
Forming limit strain
Strain distribution
In-plane stretching
Out-of-plane stretching

## Slide 6: Punch-die assembly for punch stretching experiments

## Slide 7
Limiting dome height test of parent metal with blank holding force of 12-15 tonnes with data acquisition system for load-displacement graph in 100 ton hydraulic press.
Lever for blank holder movement
Lever for Punch movement
Blank holder pressure gauge
hemispherical Punch
Upper die
Lower die
Load cell
Blank holder

## Slide 8
Stretch formed specimens

## Slide 10
Forming limit diagram
Or
Forming limit curve

## Slide 11
Laboratory scale formability testing facility developed at IIT KGP
100 ton double action press
Limiting dome height test rig
Stretch formed specimens in different strain path till failure
The ability to distribute strain over an arbitrary tool surface is a complex interaction of mechanical properties, tool design and process parameters.
Design variables
Draw-bead size, Die corner radius, Punch corner radius, Punch-die clearance
Process variables
Mode of stretching, Strain path, Temperature, Deformation speed, Blank holding pressure, Lubrication.
4

## Slide 12
FLD as failure diagnostic tool in sheet metal stamping industries
Forming Limit Diagram: Measure of formability
Limiting surface strain
Tension-tension region
Tension-compression region
FLD0
5

## Slide 13
At constant strain
Tensile properties we are investigating
High m-value promotes large deformation
3

## Slide 14: Deep Drawing
wrinkling
Fracture at die corner
Fracture at punch corner
earing

## Slide 16
Material | R0 | R45 | R90 |  | ΔR
IF Steel | 2.12 | 1.73 | 2.47 | 2.01 | 0.565
RD
Lankford Anisotropy Coefficient
Normal Anisotropy
Planar Anisotropy
Hill’s(1948) Yield Function for Plane Stress
For isotropy,
1
Experiment | Hill’s | von-Mises
Anisotropy measurement and Earring prediction
6

## Slide 17
Improvement in Deep Drawing Behavior of Anisotropy Steel
1.The ΔR1 and ΔR2 were
obtained as,
ΔR1= R0 - R45
ΔR2 = R90 - R45
2.Modified X-Coordinate
= R- β ΔR1
Modified Y-Coordinate
= R- β ΔR2
3. Modified blank 1 for β=6.
Modified blank 2 for β=5.
Modified blank 3 for β=4
Initial blank shape modification to minimize earring
Improvement in deep drawing behavior
Metal flow analysis
7