## Slide 1
hot hardness
thermal shock resistance
chemical stability
abrasion wear resistance
toughness
properties of cutting
tool materials

## Slide 2
HSS
sintered tungsten carbide
cermets - TiC
ceramics
cBN
diamond
coated tools
  coated HSS
  coated carbides
  hard coating – TiN, TiC, TiCN, Al2O3, TiAlN, cBN, diamond
  soft coating – MoS2, WS2
  hybrid coating – metal nitride + metal sulphide

## Slide 3
high speed steel

## Slide 4
for machining cast iron, non-ferrous materials, Ti- and Ni- based superalloys
  WC+Co
  K grade – K01 to K40
for machining cast steels
  M grade – M10 to M40
for machining steel
  WC+Co+TiC+TaC+NbC
  P grade – P01 to P40
micro-crystalline grade – grain size of WC less than 1 m (typically 0.8 m)

## Slide 5
cermets – ceramic + metal
  TiC, TiN, TiCN + Ni, Co, Ni-Co, Ni-Mo, Fe
ceramics
  oxide (Al2O3) and nitride (Si3N4)ceramics
  toughening is essential
    partially stabilised zirconia,
    silver
    SiC whiskers toughened
  SIALON (Si3N4 + Al2O3)

## Slide 6
coated tools
  coated HSS
  coated carbides
  hard coating – TiN, TiC, TiCN, Al2O3, TiAlN, cBN, diamond
  soft coating – MoS2, WS2
  hybrid coating – metal nitride + metal sulphide
  lubricating coating – TiN, MoS2, WS2, DLC
technology
  CVD
  PVD
  HF-CVD for diamond coating