## Slide 1: X-Ray Diffraction
Diffraction gratings must have spacings comparable to the wavelength of diffracted radiation.
Can’t resolve spacings  
Spacing is the distance between parallel planes of atoms.

## Slide 2: f19_03_pg68
Notes: f19_03_pg68.jpg

## Slide 3: f20_03_pg69
Notes: f20_03_pg69.jpg

## Slide 4: f21_03_pg70
Notes: f21_03_pg70.jpg

## Slide 5: X-Ray Diffraction Pattern
(110)
(200)
(211)
z
x
y
a
b
c
Diffraction angle 2q
Diffraction pattern for polycrystalline a-iron (BCC)
Intensity (relative)
z
x
y
a
b
c
z
x
y
a
b
c

## Slide 6: Imperfections in Solids
There is no such thing as a perfect crystal.
What are these imperfections?
Why are they important?
Many of the important properties of materials are due to the presence of imperfections.

## Slide 7: Types of Imperfections
• Vacancy, Self interstitials
• Impurity atoms
  Interstitial
  Substitutional
Point defects
• Dislocations
Line defects
• Grain Boundaries,
Stacking Faults,
Twin Boundaries
Anti Phase Boundaries
Area defects
• Pores, blow holes
Pin holes
Volume defects

## Slide 8: Point Defects
• Vacancies:
-vacant atomic sites in a structure.
• Self-Interstitials:
-"extra" atoms positioned between atomic sites (voids).

## Slide 9: Equilibrium Concentration: Point Defects
Boltzmann's constant
(1.38 x 10
-23
J/atom-K)
(8.62
x
10
-5
eV/atom-K)
ç
N
v
N
=
exp
-
Q
v
k
T
æ
è
ç
ö
ø
No. of defects
No. of potential
defect sites.
Activation energy
Temperature
Each lattice site
is a potential
vacancy site
• Equilibrium concentration varies with temperature!
For most metals, the fraction of vacancies Nv/N just below the melting temperature is on the order of 104; that is, one lattice site out of 10,000 will be empty

## Slide 10: Measuring Activation Energy
• We can get Qv from
an experiment.
ç
÷
N
v
N
=
exp
-
Q
v
k
T
æ
è
ç
ö
ø
÷
• Measure this...
N
v
N
T
exponential
dependence!
defect concentration
• Replot it...
1/
T
N
N
v
ln
-
Q
v
/k
slope

## Slide 11: Estimating Vacancy Concentration
• Find the equil. # of vacancies in 1 m3 of Cu at 1000C.
• Given:
A
Cu
= 63.5 g/mol
r
= 8.4 g
/
cm
3
Q
v
= 0.9 eV/atom
N
A
= 6.02 x 1023
atoms/mol
For 1 m3
, N =
N
A
A
Cu
r
x
x
1 m3
= 8.0 x 1028 sites
8.62 x 10-5
eV/atom-K
0.9 eV/atom
1273K
ç
÷
N
v
N
=
exp
-
Q
v
k
T
æ
è
ç
ö
ø
÷
= 2.7 x 10-4
• Answer:
N
v
=
(2.7 x 10-4)(8.0 x 1028) sites = 2.2 x 1025 vacancies

## Slide 12
Diffusive migration of vacancies on Ge surface as observed through scanning tunneling microscope

## Slide 13: f02_04_pg5
Impurity Atoms
Notes: f02_04_pg5.jpg

## Slide 14: f12_20_pg434
Defects in Ceramic Structures
Notes: f12_20_pg434.jpg

## Slide 15: f12_21_pg435
• Frenkel Defect
A cation is out of place.
• Schottky Defect
A paired set of cation and anion vacancies.
Defects in Ceramic Structures
Notes: f12_21_pg435.jpg

## Slide 16: Impurities
• Impurities must also satisfy charge balance = Electroneutrality
• Ex: NaCl
• Substitutional cation impurity
Na
+
Cl
-
initial geometry
Ca
2+
impurity
resulting geometry
Ca
2+
Na
+
Na
+
Ca
2+
cation
vacancy
• Substitutional anion impurity
initial geometry
O
2-
impurity
O
2-
Cl
-
anion vacancy
Cl
-
resulting geometry

## Slide 17: f12_22_pg435
Non Stoichiometric compound
Notes: f12_22_pg435.jpg

## Slide 18: Linear (1d) defects in crystals: Dislocations Non-equilibrium defects and would leave the crystal if given an opportunity.

## Slide 19
Slip
Role of Dislocations
Fracture
Fatigue
Creep
Diffusion (Pipe)
Structural
Grain boundary (low angle)
Incoherent Twin
Semicoherent Interfaces
Disc of vacancies ~ edge dislocation
Deformation Processes
Crystal Growth (Screw dislocation)
Kinetics
Note: Structural dislocations can also play a role in deformation and kinetic processes
and more…!!
Creep
mechanisms in
crystalline
materials
Dislocation climb
Vacancy diffusion
Cross
-
slip
Grain boundary sliding

## Slide 20
Slipped part of the crystal
Unslipped part of the crystal
Dislocation can be considered as a boundary between the slipped and the unslipped parts of the crystal lying over a slip plane*
* this is just a way of visualization and often the slipped and unslipped regions may not be distinguished

## Slide 21
A dislocation has associated with it two vectors:
The Burgers vector is the shortest lattice translation vector for a full/perfect dislocation)
It defines every aspect of the dislocation (its stress fields, energy, etc.) and expresses itself even in the ‘death’ of the dislocation (i.e. when the dislocation leaves the crystal and creates a step of height ‘b’).
Burgers vector can be determined by the Burgers circuit (coming up).

## Slide 22
Some models of Edge Dislocation
Model using magnetic balls (not that accurate!)

## Slide 23
Edge dislocation
Often to visualize the edge dislocation, only the extra ‘half’-plane and slip plane are shown. The remaining crystal is hidden away.
The intersection of the extra half-plane and slip plane can be visualized as the dislocation line.

## Slide 24: Screw Dislocation
Screw Dislocation
Burgers vector b
Dislocation
line
b
(a)
(b)
Comprises a structure in which a helical path is traced around the linear defect (dislocation line) by the atomic planes of atoms in the crystal lattice

## Slide 25
A Burgers circuit in a crystal containing dislocations is an atom-to-atom
path which forms a closed loop. -- in Fig. 1.19(a), MNOPQ.
If the same atom-to-atom sequence is made in a dislocation free crystal, Figure 1.19(b), and the circuit does not close, then the first circuit, Fig. 1.19(a), must enclose one or more dislocations.
The vector required to complete the circuit is called the Burgers vector.
Burgers circuit
Edge dislocation

## Slide 26
Screw dislocation
Burgers circuit
When the Burgers circuit is drawn round a screw dislocation (Fig. 1.20), with a closed circuit in the crystal containing the dislocation,
Closure failure in the perfect crystal is given by vector QM
Burgers vector QM is parallel to the dislocation line.

## Slide 27
Rules for construction of Burgers circuit
When looking along the dislocation line, which defines the positive line sense or direction of the dislocation, the circuit is taken in a clockwise fashion (Figs 1.19(a), 1.20(a)).
The Burgers vector is taken to run from the finish to the start point of the reference circuit in the perfect crystal.
This defines the right-hand/finish start (RH/FS) convention.

## Slide 28
Looking down the dislocation line, if the helix advances one plane when a clockwise circuit is made round it (Fig. 18(d)), it is referred to as a right-handed screw dislocation, and if the reverse is true it is left-handed.
Right-handed screw dislocation
Left-handed screw dislocation

## Slide 29
More about Burgers vector
Reversing the line sense reverses the direction of the Burgers vector for a given dislocation.
Dislocations with the same line sense but opposite Burgers vectors (or alternatively with opposite line senses and the same Burgers vector) are physical opposites, in that if one is a positive edge, the other is a negative edge, and if one is a right handed screw, the other is left-handed.
Dislocations which are physical opposites of each other annihilate and restore perfect crystal if brought together.

## Slide 30
TEM image of edge dislocation in Cu crystal. The Burgers circuit around the dislocation line can be clearly observed.

## Slide 31
Geometric properties of dislocations
Dislocation Property | Type of dislocation | 
 | Edge | Screw
Relation between dislocation line (t) and b |  | ¦¦
Slip direction** (& the ‘direction’ of step created when dislocation leaves the crystal) | ¦¦ to b | ¦¦ to b
Direction of dislocation line movement relative to b | ¦¦ | 
Process by which dislocation may leave slip plane* | climb | Cross-slip
In a edge dislocation : b is perpendicular to t.
In a screw dislocation : b is parallel to t.
Other properties are as in the table below.
* Note: edge dislocations cannot cross slip & screw dislocations cannot climb.
** Slip is the end result when dislocation leaves the crystal to create a step. Slip is hence always parallel to b.

## Slide 32
Climb
Cross slip

## Slide 33: Edge, Screw, and Mixed Dislocations
Edge
Screw
Mixed

## Slide 34
TEM image of curved dislocation line with mixed character.

## Slide 35
A dislocation whose Burgers vector is a lattice translation vector is known as a perfect or unit dislocation.
Dislocations tend to have as small a Burgers vector as possible.
Dislocations are non-equilibrium defects and would leave the crystal if given an opportunity.

## Slide 36: Line Defects
• slip between crystal planes result when dislocations move
• produce permanent (plastic) deformation.
Dislocations:
Schematic of Zinc (HCP):
• before deformation
• after tensile elongation
slip steps

## Slide 37: Characterization of dislocations
Dislocations are visible in electron micrographs
Dislocations can be observed using transmission electron microscopy, field ion microscopy, scanning tunneling microscopy and atom probe techniques

## Slide 38: Planar Defects
External Surface
Grain Boundary
Twin Boundary
Phase Boundary
Stacking Fault
Domain Boundary
Anti Phase Boundary

## Slide 39
Crystals of different orientations meet.
A single-phase interface, with crystals on each side of the boundary being identical except in orientation.
Grain Boundary

## Slide 40: Twin Boundary
  Essentially a reflection of atom positions across the twin plane
Twinned structure : Typical characteristics – always parallel lines are present

## Slide 41
ABCABACABCA...
ABCABABCA...
ABCABCABCA...
"intrinsic stacking fault“
Removal of layer C
"extrinsic stacking fault“
Insertion of layer A
Stacking Fault

## Slide 42
HRTEM (high-resolution TEM) image shows the atomic structure of planar defects in thin-film silicon:
a twin defect
an intrinsic stacking fault (ISF)
an extrinsic stacking fault (ESF—in which there is an intervening layer between two layers slightly shifted from each other)
HRTEM image of defects

## Slide 43
occur in ordered alloys
The crystallographic direction remains the same
If the ordering is usually ABABABAB, an anti phase boundary takes the form of ABABBABA.
Anti Phase Boundary

## Slide 44
Voids are small regions where there are no atoms, and can be thought of as clusters of vacancies.
Impurities can cluster together to form small regions of a different phase. These are often called precipitates.
Cracks, other phases also fall in this category.
Bulk defects

## Slide 45
Volume defects

## Slide 46: f14_15_pg515
Imperfections in Polymers
Notes: f14_15_pg515.jpg

## Slide 48: Optical Microscopy
• Useful up to 2000X magnification.
• Polishing removes surface features (e.g., scratches)
• Etching changes reflectance, depending on crystal
orientation.
Micrograph of
brass (a Cu-Zn alloy)
crystallographic planes

## Slide 49: Optical Microscopy
Grain boundaries...
• are imperfections,
• are more susceptible
to etching,
• may be revealed as
dark lines,
• change in crystal
orientation across
boundary.
ASTM grain
size number
N
= 2
n
-1
number of grains/in2
at 100x
magnification

## Slide 50: Microscopy
Optical resolution ca. 10-7 m = 0.1 m = 100 nm
For higher resolution need higher frequency
  Electrons
    Wavelengths ca. 3 pm (0.003 nm)
    Atomic resolution possible
    Electron beam focused by magnetic lenses.

## Slide 51: f15a_04_pg102
Notes: f15a_04_pg102.jpg

## Slide 52: Next Topic
Deformation and Strengthening Mechanisms