## Slide 2: f07_03_pg54
3-indices (Miller indices) and
4-indices (Miller–Bravais indices), coordinate system
Directions in Hexagonal Crystal
Notes: f07_03_pg54.jpg

## Slide 3: Indexing of Crystallographic directions in hexagonal system
Four Index system:
  Indexing algorithm is same as cubic system.
  Take perpendicular projections on the axes
Three Index system:
  Projections should be in hexagonal co-ordinate system reference frame

## Slide 4: p_pg55
What is this direction CF?
1 1 -2 3
Finding perpendicular projections in Hexagonal crystal system is not always convenient
In three index system: [1 1 1]
Notes: p_pg55.jpg

## Slide 5: 3 index to 4 index
Why we need 4 index system?
In 4 index system, Indices reveal crystallographically equivalent directions

## Slide 6: 3 index (Miller indices) to 4 index (Miller-Bravais indices)
Hexagonal Crystals
  4 parameter Miller-Bravais lattice coordinates are related to the direction indices (i.e., u'v'w') as follows.
=
=
=
'
w
w
t
v
u
)
v
u
(
+
-
)
'
u
'
v
2
(
3
1
-
)
'
v
'
u
2
(
3
1
-
=
]
uvtw
[
]
'
w
'
v
'
u
[
®
-
a3
a1
a2
z

## Slide 7: p_pg55
1 1 -2 3
In Four index system:
What is the index of the direction CE?
Notes: p_pg55.jpg

## Slide 12: Bravais Lattices
Named after named after Auguste Bravais
7 Crystal Systems
Centering
14 Bravais Lattices
Primitive
Body Centering
Face Centering
Base Centering

## Slide 14: Bravais Lattices (14)

## Slide 16: f03_03_pg43
Hexagonal unit cell
HCP Structure
Notes: f03_03_pg43.jpg

## Slide 17: f13_03_pg62
Atomic layer arrangement
Notes: f13_03_pg62.jpg

## Slide 18: f14_03_pg62
Hexagonal packing
Notes: f14_03_pg62.jpg

## Slide 19: HCP

## Slide 21
HCP : ideal c/a ratio is 1.633

## Slide 22
A sites
B
B
B
B
B
B
B
C
sites
C
C
C
A
B
B
sites
• ABCABC... Stacking Sequence
• 2D Projection
• FCC Unit Cell
Stacking Sequence
C
C
C
A
C
C
C
A
A
B
C

## Slide 23: f15_03_pg63
Cubic closed packing
Notes: f15_03_pg63.jpg

## Slide 24: f01_03_pg40
FCC unit cell
BCC unit Cell
Notes: f01_03_pg40.jpg

## Slide 25
http://www.chemtube3d.com/solidstate/_table.htm

## Slide 26: Atoms Per Unit Cell
Corners - shared by eight unit cells (x 1/8)
Edges - shared by four unit cells (x 1/4)
Faces - shared by two unit cells (x 1/2)

## Slide 27: Common Metal Structures
Face-Centered Cubic (FCC)
  8 corners x 1/8 + 6 faces x 1/2
  1 + 3 = 4 atoms/u.c.
Body-Centered Cubic (BCC)
  8 corners x 1/8 + 1 center
  1 + 1 = 2 atoms/u.c.
Hexagonal Close-Packed (HCP)
  4 corners x 1/6 + 4 corners x 1/12 + 1 middle
  2/3 +1/3 + 1 = 2 atoms/u.c.

## Slide 29: Simple Cubic Structure (SC)
• Rare due to low packing density (only Po has this structure)
• Close-packed directions are cube edges.
• Coordination # = 6
(# nearest neighbors)

## Slide 30: Atomic Packing Factor (APF)
• APF for a simple cubic structure = 0.52
APF =
a
3
4
3
p
(0.5a)
3
1
atoms
unit cell
atom
volume
unit cell
volume
APF =
Volume of atoms in unit cell*
Volume of unit cell
*assume hard spheres

## Slide 31: Body Centered Cubic Structure (BCC)
• Coordination # = 8
• Atoms touch each other along cube diagonals.
--Note: All atoms are identical; the center atom is shaded
differently only for ease of viewing.
ex: Cr, W, Fe (), Tantalum, Molybdenum
2 atoms/unit cell: 1 center + 8 corners x 1/8

## Slide 32: Atomic Packing Factor: BCC
a
APF =
4
3
p
(
3
a/4
)
3
2
atoms
unit cell
atom
volume
a
3
unit cell
volume
length = 4R =
Close-packed directions:
3 a
• APF for a body-centered cubic structure = 0.68
a
2
a
3

## Slide 33: Face Centered Cubic Structure (FCC)
• Coordination # = 12
• Atoms touch each other along face diagonals.
--Note: All atoms are identical; the face-centered atoms are shaded
differently only for ease of viewing.
ex: Al, Cu, Au, Pb, Ni, Pt, Ag
4 atoms/unit cell: 6 face x 1/2 + 8 corners x 1/8

## Slide 34: Atomic Packing Factor: FCC
• APF for a face-centered cubic structure = 0.74
maximum achievable APF
APF =
4
3
p
(
2
a/4
)
3
4
atoms
unit cell
atom
volume
a
3
unit cell
volume
Close-packed directions:
length = 4R =
2 a
Unit cell contains:
6 x 1/2 + 8 x 1/8
=
4 atoms/unit cell

## Slide 35
APF =
4
3
p
(
R
)
3
2
atoms
unit cell
atom
volume
3/2 a c
2
unit cell
volume
Close-packed directions:
length = 2R =
a
Unit cell contains:
4 x 1/(3 x 2) + 4 x 1/(6 x 2) + 1
=
2 atoms/unit cell
c/a =( 8/3 )
Atomic Packing Factor: HCP

## Slide 36: Theoretical Density, r
where n = number of atoms/unit cell
A = atomic weight
VC = Volume of unit cell = a3 for cubic
NA = Avogadro’s number
= 6.023 x 1023 atoms/mol
Density =  =
VC NA
n A
 =
Cell
Unit
of
Volume
Total
Cell
Unit
in
Atoms
of
Mass

## Slide 37: Theoretical Density, r
Ex: Cr (BCC)
A = 52.00 g/mol
R = 0.125 nm
n = 2
theoretical
a = 4R/ 3 = 0.2887 nm
ractual
 =
a
3
52.00
2
atoms
unit cell
mol
g
unit cell
volume
atoms
mol
6.023 x 1023
= 7.18 g/cm3
= 7.19 g/cm3

## Slide 39: Linear Density
ex: linear density of Al in [110] direction a = 0.405 nm
Linear Density of Atoms  LD =
Unit length of direction vector
Number of atoms
# atoms
length
1
3.5 nm
a
2
2
LD
-
=
=

## Slide 40: Planar Density of (100) Iron
At T < 912C iron has the BCC structure.
(100)
Radius of iron R = 0.1241 nm
R
3
3
4
a
=
2D repeat unit
=
Planar Density =
a
2
1
atoms
2D repeat unit
=
nm2
atoms
12.1
m2
atoms
= 1.2 x 1019
1
2
R
3
3
4
area
2D repeat unit

## Slide 41: Planar Density of (111) Iron
Solution (cont): (111) plane
1 atom in plane/ unit surface cell
3
3
3
2
2
R
3
16
R
3
4
2
a
3
ah
2
area
=
÷
÷
ø
ö
ç
ç
è
æ
=
=
=
atoms in plane
atoms above plane
atoms below plane
a
h
2
3
=
a
2
2D repeat unit
1
=
=
nm2
atoms
7.0
m2
atoms
0.70 x 1019
3
2
R
3
16
Planar Density =
atoms
2D repeat unit
area
2D repeat unit

## Slide 43: Octahedral interstitial sites
FCC
BCC
The space in the interstices between 6 regular atoms that form an octahedron.
Four regular atoms are positioned in a plane, the other two are in a symmetrical position just above or below.
12/4 +1 = 4 positions per unit cell
12/4 + 6/2 = 6 positions per unit cell

## Slide 44: Tetrahedral interstitial sites
FCC
BCC
The center of a tetrahedra formed by four lattice atoms.
Three atoms, touching each other, are in plane; the fourth atom sits in the symmetrical position on top.
8 positions per unit cell
(6 · 4)/2 = 12 positions per unit cell