## Slide 1
http://www.chemtube3d.com/solidstate/_table.htm

## Slide 3: Ceramic Crystal Structures

## Slide 4: t12_01_pg416
Bond characters of ceramics
where XA&XB are Pauling electro-negativities
For ceramic materials with predominantly ionic character, crystal structure is composed of cations and anions
Two characteristics of these ions influence the crystal structure
  The magnitude of electrical charge (Charge balance must be there)
  Relative sizes (Each cation/ anion prefers to have as many nearest neighbour anions/ cations as possible)
Notes: t12_01_pg416.jpg

## Slide 5: f12_01_pg416
Radius Ratio Rules
Stable ceramic crystal structure forms when those anions surrounding a cation are all in contact with that cation
The coordination number (number of anion nearest neighbours for a cation) is related to the cation anion radius ratio
For a specific coordination number, there is a critical or minimum rC/rA ratio for which this cation-anion contact is established
Notes: f12_01_pg416.jpg

## Slide 6: t12_02_pg417
Radius Ratio Rules
Some points about ionic size:
Cation< atom < anion
Cation with higher positive charge are smaller
As coordination number increases, cation size increases
Notes: t12_02_pg417.jpg

## Slide 7: f_pg419
Minimum rC/rA ratio for CN=3
Notes: f_pg419.jpg

## Slide 8: t12_04_pg422
Common Ceramic Crystal Structures
FCC
SC
Notes: t12_04_pg422.jpg

## Slide 9: Crystal = Bravais lattice + Base
A crystal is obtained by taking a Bravais lattice and adding a base! The base can just be one atom (as in the case of many elemental crystals, most noteworthy the metals), two identical atoms (e.g. Si, Ge, C(diamond)), two different atoms (NaCl, GaAs, ...) three atoms, ... up to huge complex molecules as in the case of protein crystals.

## Slide 10: f12_02_pg420
Rock Salt (NaCl) Structure
(fcc), with two atoms in the base: one at (0, 0, 0), the other one at (½, ½, ½)
Many salts and oxides have this structure, e.g. KCl, AgBr, KBr, PbS, ... or MgO, FeO, ...
Notes: f12_02_pg420.jpg

## Slide 11: f12_03_pg420
CsCl Crystal Structure
cubic primitive with two atoms in the base at (0,0,0) and (½, ½, ½)
Intermetallic compounds (not necessarily ionic crystals), but also common salts assume this structure; e.g. CsCl, ..., or AlNi, CuZn
Notes: f12_03_pg420.jpg

## Slide 12: f12_04_pg421
ZnS (Zinc Blende) Structure
(fcc) with two atoms in the base at (0,0,0) and (¼, ¼, ¼)
typical lattice of covalently bonded group IV semiconductors (C (diamond form), Si, Ge) or III-V compounds semiconductors (GaAs, GaP, InSb, InP, ..)
Notes: f12_04_pg421.jpg

## Slide 13: f12_05_pg421
CaF2 (Fluorite) Structure
(fcc) with three atoms in the base, one kind (the cations) at (0,0,0), and the other two (anions of the same kind) at (¼, ¼, ¼), and (-¼, -¼, -¼)
Notes: f12_05_pg421.jpg

## Slide 14: f12_06_pg422
Perovskite crystal Structure
cubic primitive:
three different atoms in the base. In the example it would be Ba at (0,0,0), O at (½, ½, ,0), at (½, 0, ½), at (0, ½, ½) and Ti at (½, ½, ½).
Barium titanate (BaTiO3), having both Ba2+ and Ti4+ cations
Notes: f12_06_pg422.jpg

## Slide 15: f12_02_pg420
Rock Salt (NaCl) Structure
Notes: f12_02_pg420.jpg

## Slide 16: f12_07_pg423
Close Packed Structure in ceramics
Close packed planes of anions
Cations reside at Tetrahedral and/ or Octrahedral interstitial sites
Notes: f12_07_pg423.jpg

## Slide 17: f12_08_pg424
Rock Salt (NaCl) Structure
Close packed arrangement of Cl ions on {111} planes
Na+ ions are at Octahedral sites
Notes: f12_08_pg424.jpg

## Slide 18: DENSITY COMPUTATIONS—CERAMICS

## Slide 19: f_pg425
DENSITY COMPUTATIONS—CERAMICS
n’ = 4; FCC lattice
Experimental value: 2.16 gm/cc
Notes: f_pg425.jpg

## Slide 20: f12_09_pg426
Silicate Ceramics
Soils, rocks, clays, and sand come under the silicate classification
Characterize crystal structure in terms of various arrangements of an SiO44- tetrahedron
Basic unit of the silicates
Notes: f12_09_pg426.jpg

## Slide 21: f12_10_pg427
Chemically, the most simple silicate
Structurally, it is a 3d network generated when every corner O atom in each tetrahedron is shared by adjacent tetrahedra.
Electrically neutral
The ratio of Si to O atoms is 1 : 2, as indicated by the chemical formula.
Silica (SiO2)
Three primary polymorphic crystalline forms of silica: quartz, cristobalite and tridymite.
Strong Si-O bonds  high mp
Relatively open str.  Low density
Notes: f12_10_pg427.jpg

## Slide 22: f12_11_pg428
Silicon dioxide (or silica, SiO2) in the noncrystalline state is called fused silica, or vitreous silica
Other oxides (e.g., B2O3 and GeO2) may also form glassy structures
SILICA GLASSES
Network formers
The common inorganic glasses used for containers  Silica glasses to which have been added other oxides such as CaO and Na2O
Cations are incorporated within and modify the SiO44- network
Network modifiers
structure of a sodium–silicate glass
Lowers the mp and viscosity of glasses  easy formation at low temp
Notes: f12_11_pg428.jpg

## Slide 23: f12_13_pg429
A 2d sheet or layered structure
By sharing of 3 O ions in each of the tetrahedra
Repeating unit formula: (Si2O5)2-
A second planar sheet structure having an excess of cations  Charge neutrality
Sheet or layered silicates
Their basic structure is characteristic of clays and other minerals
Notes: f12_13_pg429.jpg

## Slide 24: f12_14_pg430
Keolinite (Clay):
2 layer silicate sheet structure
Al2(Si2O5)(OH)4
Talc
Mica
Notes: f12_14_pg430.jpg

## Slide 25: f12_15_pg431
Diamond Cubic Structure
Extremely hard
Low electrical conductivity
Optically Transparent
High index of refraction
Notes: f12_15_pg431.jpg

## Slide 26: f12_17_pg432
Graphite
Lubricative property
Electrical conductivity along sheet
Notes: f12_17_pg432.jpg

## Slide 27: f12_18_pg432
Fullerenes
Exists in molecular form
C60
Each molecule called Buckyball
Material consisting of C60 molecules are called Buckminsterfullerene or Fullerene
Notes: f12_18_pg432.jpg

## Slide 28: f12_19_pg433
Carbon Nanotube
Single sheet of graphite rolled into a tube. Both ends are C60 hemispheres
Notes: f12_19_pg433.jpg

## Slide 29: f14_12_pg513
Chain Folded model of Polymer crystallite
Notes: f14_12_pg513.jpg

## Slide 30: f14_13_pg513
Spherulite sructure
Notes: f14_13_pg513.jpg

## Slide 31: Single vs Polycrystals
• Single Crystals
-Properties vary with
direction: anisotropic.
-Example: the modulus
of elasticity (E) in BCC iron:
• Polycrystals
-Properties may/may not
vary with direction.
-If grains are randomly
oriented: isotropic.
(Epoly iron = 210 GPa)
-If grains are textured,
anisotropic.
200 mm
E (diagonal) = 273 GPa
E (edge) = 125 GPa

## Slide 32: f16_03_pg64
Notes: f16_03_pg64.jpg

## Slide 33: f17_03_pg65
Concept of Grains and Grain Boundary: Single crystal vs. polycrystalline
Notes: f17_03_pg65.jpg