## Slide 1: Fundamentals of Plastic Deformation of Metals

## Slide 2: Elastic Deformation vs Plastic Deformation
Metallic materials may experience two kinds of deformation: Elastic and Plastic
  Nonpermanent: When the applied load is released, the piece returns to its original shape
  Permanent
  On an atomic scale, Small changes in the interatomic spacing and the stretching of interatomic bonds
  Net movement of large numbers of atoms in response to an applied stress. Interatomic bonds must be ruptured and then reformed.
1
2

## Slide 3: Elastic Deformation vs Plastic Deformation
  Elastic modulus or stiffness is the material’s resistance to elastic deformation. The greater the modulus, the stiffer the material, or the smaller the elastic strain that results from the application of a given stress.
  Strength and hardness are measures of a material’s resistance to plastic deformation.
3

## Slide 4: Plastic Deformation
Plastic deformation corresponds to the motion of large numbers of dislocations.
Let’s see what happens when one dislocation is created and moves

## Slide 5
Generation of an edge dislocation by a shear stress
Movement of the dislocation through the crystal
Shift of the upper half of the crystal after the dislocation emerged
Dislocation Motion

## Slide 6: Dislocation Motion
Dislocations & plastic deformation
Plastic deformation by plastic shear or slip where one plane of atoms slides over adjacent plane by defect motion (dislocations).
If dislocations don't move, deformation doesn't occur!

## Slide 7: f03_07_pg177
Analogy between caterpillar and dislocation motion
Notes: f03_07_pg177.jpg

## Slide 8: f02_07_pg177
Dislocation Motion
The formation of a step on the surface of a crystal by the motion of
(a) an edge dislocation
The dislocation line moves in the direction of the applied shear stress
The dislocation line motion is perpendicular to the stress direction.
(b) a screw dislocation
The direction of motion of the mixed dislocation line is neither perpendicular nor parallel to the applied stress, but lies somewhere in between
Notes: f02_07_pg177.jpg

## Slide 9: Dislocation Density
Dislocations are introduced during solidification, during plastic deformation, and as a consequence of thermal stresses that result from rapid cooling.
Dislocation density is expressed as the total dislocation length per unit volume, or, equivalently, the number of dislocations that intersect a unit area of a random section.
The units of dislocation density are millimeters of dislocation per cubic millimeter or just per square millimeter.

## Slide 10: Dislocation Density
Carefully solidified metal crystals: 103 mm-2
Heavily deformed metals: 109 to 1010 mm-2.
(Important source of these new dislocations: 1) existing dislocations, which multiply; 2) grain boundaries, 3) internal defects and surface irregularities such as scratches and nicks, which act as stress concentrations)
Heat treating a deformed metal specimen can diminish the density to on the order of 105 to 106 mm-2.
Ceramic materials: 102 - 104 mm-2
Silicon single crystals used in integrated circuits:
0.1 -1 mm-2.

## Slide 11: f04_07_pg178
Strain Energy
When metals are plastically deformed, some fraction of the deformation energy (approximately 5%) is retained internally; the remainder is dissipated as heat.
The major portion of this stored energy is as strain energy associated with dislocations.
Notes: f04_07_pg178.jpg

## Slide 12: f05_07_pg179
Important in the strengthening mechanisms for metals.
Strain fields and associated forces
Notes: f05_07_pg179.jpg

## Slide 13: Dislocation Movement and Slip
There are two basic types of dislocation movements:
  Glide: Dislocation moves in the plane which contains both its line and Burgers vector
  Climb: Dislocations moves out of the glide plane normal to the Burgers vector
Glide of many dislocations result in Slip
Slip: Most common manifestation of plastic deformation in crystalline solids

## Slide 14: Slip System: Slip Plane + Slip Direction
Glide of dislocations occurs not with same degree of easiness on all crystallographic planes of atoms and in all crystallographic directions.
Preferred plane, and in that plane specific directions along which dislocation glide occurs.
This plane is called the slip plane;
The direction of movement is called the slip direction.
This combination of the slip plane and the slip direction is termed the slip system.

## Slide 15: Slip System: Slip Plane + Slip Direction
The slip system depends on the crystal structure of the metal and is such that the atomic distortion that accompanies the motion of a dislocation is a minimum.
For a particular crystal structure, the slip plane is that plane having the most dense atomic packing
The slip direction corresponds to the direction, in this plane, that is most closely packed with atoms, that is, has the highest linear density.

## Slide 16: f06_07_pg180
Slip System in FCC
There are 4 close-packed planes {111} with 3 close-packed directions in each plane < 110 >
– a total of 12 slip systems.
Slip occurs along <110>-type directions within the {111} planes
{111}<110> represents the slip plane and direction combination, or the slip system for FCC.
Notes: f06_07_pg180.jpg

## Slide 18: Slip Systems in BCC
No close-packed plane, but close-packed directions < 111 >
Three types of planes which are nearly tied for the highest packing density.
near close - packed planes in BCC : {110} {321} {211}
All these planes have been observed to be slip planes.
Thus we have the following slip systems in BCC crystals:
• 6 {110} planes each with 2 < 111 > directions = 12 slip systems
• 24 {321} planes each with 1 < 111 > direction = 24 slip systems
• 12 {211} planes each with 1 < 111 > direction = 12 slip systems

## Slide 19: Slip Systems in HCP
The basal plane (0001) is the close-packed plane and there are 3 close-packed directions < 1120 >
There can be other slip systems in HCP called Prism slip {1010} and Pyramid slip {1011}. Slip direction will remain the close packed <1120> direction

## Slide 20: Slip System for FCC, BCC and HCP Metals
FCC or BCC: Relatively large number of slip systems (at least 12).
These metals are quite ductile because extensive plastic deformation is normally possible along the various systems.
HCP metals, having few active slip systems, are normally quite brittle.

## Slide 21: Slip in a single crystal
slip plane
normal, ns
Resolved shear
stress:
tR
=
F
s
/A
s
slip
direction
AS
tR
tR
FS
Applied tensile
stress:
= F/A
s
slip
direction
F
A
F
slip
direction
tR
=
FS
/AS
F
cos
l
A
/
cos
f
l
F
FS
f
nS
AS
A
Relation between
s
and
tR

## Slide 22: Deformation in Single Crystal
A metal single crystal has a number of different slip systems that are capable of operating. The resolved shear stress normally differs for each one because the orientation of each relative to the stress axis (f and l angles) also differs.
However, one slip system is generally oriented most favorably, that is, has the largest resolved shear stress, tR(max): tR(max) = s(cos f cos l)max

## Slide 23: Slip in Single Crystal
In response to an applied tensile or compressive stress, slip in a single crystal commences on the most favorably oriented slip system when the resolved shear stress reaches some critical value, termed the critical resolved shear stress tcrss
tcrss represents the minimum shear stress required to initiate slip
tcrss is a property of the material that determines when yielding occurs.
The single crystal plastically deforms or yields when tR(max) = tcrss

## Slide 24: Slip in single crystal
The single crystal plastically deforms or yields when tR(max) = tcrss
The magnitude of the applied stress required to initiate yielding (i.e., the yield strength sy) is
The minimum stress necessary to introduce yielding occurs when a single crystal is oriented such that f=l=450; under these conditions, sy = 2 tcrss

## Slide 25: Critical Resolved Shear Stress
• Condition for dislocation motion:
• Crystal orientation can make
it easy or hard to move dislocation
10-4 GPa to 10-2 GPa
typically
 maximum at  =  = 45º
tR
= 0
l
=90°
s
tR
=
s
/2
l
=45°
f
=45°
s
tR
= 0
f
=90°
s

## Slide 26: Single Crystal Slip

## Slide 27: Ex: Deformation of single crystal
So the applied stress of 6500 psi will not cause the crystal to yield.
=35°
=60°
crss = 3000 psi
a) Will the single crystal yield?
b) If not, what stress is needed?
 = 6500 psi

## Slide 28: Ex: Deformation of single crystal
What stress is necessary (i.e., what is the yield stress, sy)?
So for deformation to occur the applied stress must be greater than or equal to the yield stress

## Slide 29: f12_07_pg187
Deformation by Twining
Plastic deformation in some metallic materials can occur by the formation of mechanical twins, or twinning
A shear force can produce atomic displacements such that on one side of a plane (the twin boundary), atoms are located in mirror image positions of atoms on the other side.
Notes: f12_07_pg187.jpg

## Slide 30
Deformation by Twining
The displacement magnitude within the twin region (indicated by arrows) is proportional to the distance from the twin plane.
Twinning occurs on a definite crystallographic plane and in a specific direction that depend on crystal structure.
For BCC metals, the twin plane and direction are (112) and [111], respectively

## Slide 31
Deformation by Twining
Mechanical twinning occurs in metals that have BCC and HCP crystal structures, at low temperatures, and at high rates of loading (shock loading), conditions under
which the slip process is restricted; that is, there are few operable slip systems.
The amount of bulk plastic deformation from twinning is normally small relative to that resulting from slip.
The real importance of twinning lies with the
accompanying crystallographic reorientations; twinning may place new slip systems in orientations that are favorable relative to the stress axis such that the slip process can now take place.

## Slide 32: f13_07_pg187
Comparison between Slip and Twin
Slip Ledges form
The crystallographic orientation above and below the slip plane is the same both before and after the deformation
Occurs in distinct atomic spacing multiples
Shear deformation is homogeneous
A reorientation across the twin plane
The atomic displacement for twinning is less than the interatomic separation
Notes: f13_07_pg187.jpg

## Slide 33: Slip Motion in Polycrystals
Random crystallographic orientations of the numerous grains
The direction of slip varies from one grain to another
For each grain, dislocation motion occurs along the slip system that has the most favorable orientation (i.e., the highest shear stress)
s
300 mm

## Slide 34: f11_07_pg186
During deformation, mechanical integrity and coherency are maintained along the grain boundaries  the grain boundaries usually do not come apart or open up. 
each individual grain is constrained, to some degree, in the shape it may assume
by its neighboring grains.
Equiaxed grains
Elongated grains
Even though a single grain may be favorably oriented with the applied stress for slip, it cannot deform until the adjacent and less favorably oriented grains are capable of slip also; this requires a higher applied stress level.
Deformation in polycrystals
Notes: f11_07_pg186.jpg

## Slide 35: Strengthening Mechanisms
• How do we increase strength?
• Strength is increased by making dislocation
motion difficult.
• Particular ways to increase strength are to:
--solid solution strengthening
--Strain hardening/ Work hardening/ Cold work
--precipitation hardening
--decrease grain size
ISSUES TO ADDRESS...

## Slide 36: Strengthening Mechanisms

## Slide 37: Strengthening Mechanisms :
Solid Solution Strengthening
Strain Hardening
Precipitation Hardening
Grain Boundary Strengthening

## Slide 38: Strengthening Mechanisms :
Solid Solution Strengthening
Strain Hardening
Precipitation Hardening
Grain Boundary Strengthening

## Slide 39: Stress Concentration at Dislocations
Adapted from Fig. 7.4, Callister 7e.
Strengthening by Alloying
Notes: Don’t move past one another – hardens material

## Slide 40: Strengthening by Alloying
small impurities tend to concentrate at dislocations on the “Compressive stress side”
reduce mobility of dislocation  increase strength
Adapted from Fig. 7.17, Callister 7e.

## Slide 41: Strengthening by alloying
Large impurities concentrate at dislocations on “Tensile Stress” side – pinning dislocation
Adapted from Fig. 7.18, Callister 7e.

## Slide 42: Example: Solid Solution Strengthening in Copper
• Tensile strength & yield strength increase with wt% Ni.
• Empirical relation:
• Alloying increases sy and TS.
Tensile strength (MPa)
wt.% Ni
200
300
400
0
10
20
30
40
50
Yield strength (MPa)
wt.%Ni
60
120
180
0
10
20
30
40
50

## Slide 43: Strengthening Mechanisms :
Solid Solution Strengthening
Strain Hardening
Precipitation Hardening
Grain Boundary Strengthening

## Slide 44: Strengthening through Strain hardening
• Also called Work hardening
Also termed as Cold working: Because, the temperature at which deformation takes place is ‘‘cold’’ relative to the absolute melting temperature of the metal
Most metals strain harden at room temperature
Often utilized commercially to enhance the mechanical properties of metals during fabrication procedures.
Phenomenon whereby a ductile metal becomes harder and stronger as it is plastically deformed

## Slide 45: Strengthening through Strain hardening
Common forming operations change the cross sectional area:
-Forging
A
o
A
d
force
die
blank
force
-Drawing
tensile
force
A
o
A
d
die
die
-Extrusion
ram
billet
container
container
force
die holder
die
A
o
A
d
extrusion
-Rolling
roll
A
o
A
d
roll
Percentage Cold Work

## Slide 46: f19_07_pg192
Examples
Notes: f19_07_pg192.jpg

## Slide 47: Example: Strain hardening
Low Carbon Steel

## Slide 48: Example:
Strain hardening effect on Stress-Strain Diagram

## Slide 49: Why materials strain harden?
Dislocation–dislocation strain field
On the average, dislocation–dislocation strain interactions are repulsive  The motion of a dislocation is hindered by the presence of other dislocations.
Cold work  Formation of new dislocations  The dislocation density in a metal increases
As the dislocation density increases, the resistance to dislocation motion by other dislocations becomes more pronounced.
Thus, the imposed stress necessary to deform a metal increases with increasing cold work.

## Slide 50: Strengthening Mechanisms :
Solid Solution Strengthening
Strain Hardening
Precipitation Hardening
Grain Boundary Strengthening

## Slide 51: Cutting precipitates:
When too small - dislocations can cut them:

## Slide 52: Bowing:
precipitates
slow dislocations
dislocations bow past
precipitates
y  Gb / L