## Slide 1: Strengthening Mechanisms :
Solid Solution Strengthening
Strain Hardening
Precipitation Hardening
Grain Boundary Strengthening

## Slide 2: Cutting precipitates:
When too small - dislocations can cut them:

## Slide 3: Bowing:
precipitates
slow dislocations
dislocations bow past
precipitates
y  Gb / L
L
L = inter precipitate distance
Orowan looping

## Slide 5: Precipitation strengthening:
y (ksi)
Heat Treating Time
50
40
30
no
precipitates
precipitates
form and grow
precipitates get too big, i.e. spacing (L) too large.
cutting
bowing
y  Gb / L

## Slide 6: Strengthening Mechanisms :
Solid Solution Strengthening
Strain Hardening
Precipitation Hardening
Grain Boundary Strengthening

## Slide 7: Strengthening through Grain Size Reduction
Grain boundaries are barriers to slip.
Barrier "strength” increases with increasing angle of misorientation
For high-angle grain boundaries, dislocations cannot traverse across grain boundaries
A stress concentration ahead of a slip plane in one grain may activate sources of new dislocations in an adjacent grain.

## Slide 8: Strengthening through Grain Size Reduction
• Smaller grain size: more barriers to slip
  a greater total grain boundary area to impede dislocation motion
Not valid for both very large or very fine grains
Hall-Petch Equation:

## Slide 9: How is grain size regulated?
Grain size may be regulated
by the rate of solidification from the liquid phase, and also
by Cold Work followed by an appropriate heat treatment

## Slide 10: Effects of cold work
Cold Work 
A change in grain shape and grain orientation
Strain hardening (increase in dislocation density)
Electrical conductivity and corrosion resistance may be modified

## Slide 11: Restoration of pre cold-worked state
Properties and structures may revert back to the precold-worked states by appropriate heat treatment (sometimes termed an annealing treatment).
Such restoration results from two different processes that occur at elevated temperatures:
Recovery and
Recrystallization,
followed by grain growth.

## Slide 12: Recovery
During recovery, Reduction in some of the stored internal strain energy through
  Some reduction in the number of dislocations (dislocation annihilation)
  Dislocation configurations are produced having low strain energies.
by virtue of dislocation motion (in the absence of an externally applied stress), as a result of enhanced atomic diffusion at the elevated temperature.
Driving force: Stored internal energy

## Slide 13: Low energy configuration of dislocations

## Slide 14: Recrystallization
Recrystallization is the formation of a new set of strain-free and equiaxed grains that have low dislocation densities
Even after recovery is complete, the grains still have stored strain energy.
Driving force: Stored internal energy
The new grains form as very small nuclei and grow until they completely replace the parent deformed material.

## Slide 15: Starting Material

## Slide 16: Cold Worked

## Slide 17: Heated at ~ 0.5 Tm

## Slide 18: Recrystallization

## Slide 19: Recrystallization

## Slide 20: f21a_07_pg195
Cold worked Structure
Several Stages of Recrystallization and grain growth of brass
Notes: f21a_07_pg195.jpg

## Slide 21: f21b_07_pg195
Initial stage of recrystallization
Several Stages of Recrystallization and grain growth of brass
Degree of recrystallization increases with time
Notes: f21b_07_pg195.jpg

## Slide 22: f21c_07_pg196
Partial replacement of cold worked grains by recrystallized ones
Several Stages of Recrystallization and grain growth of brass
Degree of recrystallization increases with time
Notes: f21c_07_pg196.jpg

## Slide 23: f21d_07_pg197
Complete recrystallization
Several Stages of Recrystallization and grain growth of brass
Degree of recrystallization increases with time
Notes: f21d_07_pg197.jpg

## Slide 24: Kinetics of recrystallization
Extent of Recrystallization depends on both time and temperature.
The degree (or fraction) of recrystallization increases with time
Avrami Equation
At constant temperature

## Slide 25: Kinetics of recrystallization: Example for pure Copper
At different temperatures

## Slide 26: Recrystallization temperature
Typically, it is between 0.3 Tm and 0.5 Tm
Depends on several factors:
  The amount of prior cold work
    TR is lowered as %CW increases
  The purity of the alloy.
    Recrystallization proceeds more rapidly in pure metals than in alloys. Thus, alloying raises the recrystallization temperature, sometimes quite substantially.
      For pure metals, the recrystallization temperature is normally 0.3Tm
      For some commercial alloys it may run as high as 0.7Tm.
TR = recrystallization temperature = The temperature at which recrystallization just reaches completion in 1 h.

## Slide 27: f23_07_pg198
The recrystallization temperature is lowered, and approaches a constant or limiting value at high deformations
There exists some critical degree of cold work below which recrystallization cannot be made to occur; normally, this is between 2 and 20% cold work.
Notes: f23_07_pg198.jpg

## Slide 28: Grain Growth
After recrystallization is complete, the strain-free grains will continue to grow if the metal specimen is left at the elevated temperature
Driving force: Grain boundary energy
  An energy is associated with grain boundaries. As grains increase in size, the total boundary area decreases, yielding an attendant reduction in the total energy.
Grain growth occurs by the migration of grain boundaries.
Not all grains can enlarge, but large ones grow at the expense of small ones that shrink.
Thus, the average grain size increases with time.

## Slide 29: f21d_07_pg197
Complete recrystallization
Several Stages of Recrystallization and grain growth of brass
Degree of recrystallization increases with time
Notes: f21d_07_pg197.jpg

## Slide 30: f21e_07_pg196
Grain growth at low temperature
Grain growth of brass at 580 deg C
Notes: f21e_07_pg196.jpg

## Slide 31: f21f_07_pg196
Further grain growth at higher temperature
Grain growth of brass at 700 deg C
Notes: f21f_07_pg196.jpg

## Slide 32: f24_07_pg200
Grain Growth
Boundary motion is just the short-range diffusion of atoms from one side of the boundary to the other.
The directions of boundary movement and atomic motion are opposite to each other
Notes: f24_07_pg200.jpg

## Slide 33: Grain Growth Equation
For many polycrystalline materials, the grain diameter d varies with time t according to the relationship
d0 is the initial grain diameter at t =0,
K and n are time-independent constants
The value of n is generally equal to or greater than 2.

## Slide 34
Recrystallization & Recovery:
  Recrystallization: High angle grain boundaries migrate
  Recovery: High angle grain boundaries do not migrate
Recrystallization and grain growth
  Recrystallization: Driving force stored strain energy
  Grain Growth: Driving force is the total grain boundary energy
Characteristic differences between Recovery, Recrystallization, and Grain Growth

## Slide 35: Hot Working
  Deforming at high enough temperature
  Dynamic recrystallization occurs
  Used for large deformation
  Poor surface finish - oxidation