## Slide 1
You can draw Eutectic phase diagram stating from the eutectic reaction
Liquid
α+β
α
β

## Slide 2
Other Phase Diagrams
Eutectoid
Peritectic
Peritectoid
  + 
α+  
 + L 

## Slide 3
Peritectic and Peritectoid Phase Diagrams
Peritectoid
Peritectic

## Slide 4
Eutectic
Eutectoid
Single Phase
Two solid Phases
Peritectic
Peritectoid
Single Phase
solid
Two Phases

## Slide 5
Cu-Zn : Intermediate Phases
Notes: f19_09_pg283.jpg

## Slide 6: Eutectoid & Peritectic
Cu-Zn Phase diagram
Eutectoid transition   + 
Peritectic transition  + L 

## Slide 7: Intermediate/ Intermetallic Compounds
Mg2Pb
Note: intermetallic compound forms a line - not an area - because stoichiometry (i.e. composition) is exact.
Not isomorphous with either of the components of the alloy system
Congruently melting intermediate phases  Intermetallic phase

## Slide 8: Few Principles about Phase Diagrams
One phase regions may touch each other only at single points (point of congruent transformation), never along a boundary
Adjacent one phase regions are seperated from each other by 2 phase regions involving the same 2 phases
Three 2 phase regions must originate upon three phase isotherm
Two three phase isotherms may be connected by a 2 phase region provided that there are 2 phases which are common to both of the three phase equilibria
All boundaries of 2 phase fields must project into 2 phase fields when they join a three phase isotherm

## Slide 9
Fe-Cementite Phase Diagram

## Slide 10: Iron-Carbon (Fe-C) Phase Diagram
• 2 important
points
-Eutectoid (B):
g
Þ
a
+
Fe3C
-Eutectic (A):
L
Þ
g
+
Fe3C
T(°C)
Result: Pearlite =
alternating layers of
a
and Fe3C phases
120 mm
(From Fig. 7.27, Callister Adapted Version.)
Fe3C (cementite)
1600
1400
1200
1000
800
600
400
0
1
2
3
4
5
6
6.7
L
g
(austenite)
g
+L
g
+Fe3C
a
+Fe3C
a
+
g
L+Fe3C
d
(Fe)
Co, wt% C
1148°C
a
727°C = T
eutectoid
A
S
R
4.30
g
g
g
g
R
S
0.76
C
eutectoid
B
Fe3C (cementite-hard)
a
(ferrite-soft)

## Slide 11
Growth of Pearlite colony
Notes: f28_09_pg295.jpg

## Slide 12: Hypoeutectoid Steel
Fe3C (cementite)
1600
1400
1200
1000
800
600
400
0
1
2
3
4
5
6
6.7
L
g
(austenite)
g
+L
g
+ Fe3C
a
+ Fe3C
L+Fe3C
d
(Fe)
Co , wt% C
1148°C
T(°C)
a
727°C
(Fe-C
System)
C0
0.76
proeutectoid ferrite
pearlite
100 mm
Hypoeutectoid
steel
R
S
a
w
a
=
S
/(
R
+
S
)
w
Fe3C
=
(1-
w
a
)
w
pearlite
=
w
g
pearlite
r
s
w
a
=
s
/(
r
+
s
)
w
g
=
(1-
w
a
)
g
g
g
g
a
a
a
g
g
g
g
g
g
g
g

## Slide 13: Hypereutectoid Steel
Fe3C (cementite)
1600
1400
1200
1000
800
600
400
0
1
2
3
4
5
6
6.7
L
g
(austenite)
g
+L
g
+Fe3C
a
+Fe3C
L+Fe3C
d
(Fe)
Co , wt%C
1148°C
T(°C)
a
(Fe-C
System)
0.76
Co
proeutectoid Fe3C
60 mm
Hypereutectoid
steel
pearlite
R
S
w
a
=
S
/(
R
+
S
)
w
Fe3C
=
(1-
w
a
)
w
pearlite
=
w
g
pearlite
s
r
w
Fe3C
=
r
/(
r
+
s
)
w
g
=(1-
w
Fe3C
)
Fe3C
g
g
g
g
g
g
g
g
g
g
g
g