## Slide 1
Phase Transformation

## Slide 2
Phase transformations (change of the microstructure) can be divided into three categories:
Diffusion-dependent with no change in phase composition or number of phases present (e.g. melting, solidification of pure metal, allotropic transformations, recrystallization, etc.)
Diffusion-dependent with changes in phase compositions and/or number of phases (e.g. eutectic or eutectoid transformations)
Diffusionless phase transformation - by cooperative small displacements of all atoms in structure, (e.g. martensitic transformation )
Diffusion-dependent phase transformations can be rather slow and the final structure often depend on the rate of cooling/heating.

## Slide 5
A phase transformation occurs spontaneously only when G decreases in the course of the transformation

## Slide 6
The formation of a solid nucleus leads to a Gibbs free energy change of
Free energy change per unit volume. Below Tm, it is -ve

## Slide 7: Homogeneous Nucleation & Energy Effects
r* = critical nucleus: nuclei < r* shrink; nuclei>r* grow (to reduce energy)
DGT = Total Free Energy
= DGS + DGV
Surface Free Energy- Energy needed to make an interface)
g = surface tension
Volume (Bulk) Free Energy –
releases of energy due to formation of solid
at r=r*,

## Slide 8
Homogeneous nucleation
at r=r*,
Hv=Lv is latent heat of solidification
Therefore,
Both r* and G* decrease with increasing undercooling

## Slide 9
Both r* and G* decrease with increasing undercooling

## Slide 10
Homogeneous nucleation in solid
Both r* and G* increase because of strain energy involved in solid state transformation

## Slide 11: Rate of Homogeneous nucleation
As T   T   G* 
exp(-(G*)/kT) 
 d 

## Slide 12: Rate of Homogeneous nucleation

## Slide 13
Heterogeneous nucleation

## Slide 14
Heterogeneous nucleation

## Slide 15
Heterogeneous nucleation

## Slide 16
 (degrees) →
G*hetero / G*homo →
G*hetero (0o) = 0 no barrier to nucleation
G*hetero (90o) = G*homo/2
G*hetero (180o) = G*homo no benefit
Complete wetting
No wetting
Partial wetting
Variation of S() with 

## Slide 17: Solidification: Nucleation Processes
Homogeneous nucleation
  nuclei form in the bulk of liquid metal
  requires supercooling (typically 80-300°C max)
Heterogeneous nucleation
  Nuclei form on mold wall or inoculants
  allows solidification with only 0.1-10ºC supercooling

## Slide 18: Nucleation rate

## Slide 19
= f(number of nucleation sites)
~ 1042
= f(number of nucleation sites)
~ 1026
BUT the exponential term dominates
Ihetero > Ihomo
Nucleation rate: Homogeneous vs. Heterogeneous

## Slide 22: Rate of Phase Transformation

## Slide 24
t (sec) →
T (K) →
99% = finish
Increasing % transformation


Time – Temperature – Transformation (TTT) diagram  →  phase transformation
1% = start

## Slide 25: Transformations & Undercooling
•
For transformation to occur, must cool to below 727°C
•
Eutectoid transformation (Fe-Fe3C system):
g
Þ
a
+
Fe3C
0.76 wt% C
0.022 wt% C
6.7 wt% C

## Slide 26: c11f13
Isothermal Transformation Diagrams
2 solid curves are plotted:
  one represents the time required at each temperature for the start of the transformation;
  the other is for transformation completion.
  The dashed curve corresponds to 50% completion.
  The austenite to pearlite transformation will occur only if the alloy is supercooled to below the eutectoid temperature (727˚C).
  Time for process to complete depends on the temperature.